## Slide 1: AME 585 Fracture Project 7 Final
Taeklim Kim
Samy Ousman
Henry Glover

## Slide 2
Question 1
NASA 5019A
Develop a Comprehensive Fracture Control Plan (FCP): Establishing and maintaining an FCP is crucial for human-rated spaceflight hardware to mitigate catastrophic failure risks due to flaws.
Classify Hardware Components Accurately: All parts should be evaluated and categorized as exempt, non-fracture critical (NFC), or fracture critical to determine appropriate control measures.
Implement Rigorous Verification Processes: Verification of fracture control requirements ensures that hardware meets safety and reliability standards.
Utilize Established Approaches for Specific Hardware Types: Applying proven methods for different hardware categories enhances reliability and safety.
Document Alternative Approaches Thoroughly: When deviating from standard practices, comprehensive documentation and approval are essential to maintain safety standards.
Ensure Material Traceability: Maintaining traceability of materials used in fracture-critical components is vital for quality assurance and safety.
Perform Detailed Failure Mode Evaluations: Identifying and assessing potential failure modes in hardware components help in implementing effective fracture control measures.
Apply Conservative Design Margins: Incorporating conservative design margins in fracture-critical components enhances safety and reliability.
Conduct Regular Training for Personnel: Ensuring that personnel involved in fracture control are adequately trained contributes to the effectiveness of the program.
Engage in Continuous Improvement: Regularly updating fracture control practices based on new findings and technological advancements fosters ongoing enhancement of safety measures.
NASA 5009
Establish Clear NDE Requirements: Defining specific NDE requirements for fracture-critical components ensures consistent application across programs.
Qualify NDE Procedures Rigorously: Qualification of NDE procedures is essential to validate their effectiveness in detecting critical flaws.
Determine Minimum Detectable Flaw Sizes: Establishing the smallest flaw size that NDE methods can reliably detect is crucial for accurate fracture analysis.
Apply Standard NDE Methods When Appropriate: Utilizing standard NDE methods with known capabilities simplifies the inspection process and ensures reliability.
Implement Special NDE for Complex Cases: For unique or complex components, special NDE procedures may be necessary to achieve the required detection capabilities.
Maintain Inspector Proficiency: Regular training and certification of NDE inspectors are vital to maintain high detection reliability.
Document NDE Results Systematically: Thorough documentation of NDE findings supports traceability and aids in the assessment of component integrity.
Integrate NDE into the Design Process: Incorporating NDE considerations early in the design phase facilitates the development of inspectable and reliable components.
Utilize Probability of Detection (POD) Curves: Employing POD curves helps in understanding the effectiveness of NDE methods and informs risk assessments.
Engage in Continuous NDE Technology Assessment: Regularly evaluating and adopting advancements in NDE technologies ensures the effectiveness of inspection processes.

## Slide 3
Question 2
Input
R = 2”; D = 4”
t = 0.1”
KIC = 22000 (Al 2024-T3)
FS = 1.4
KIC = 22000/1.4 = 15714
P = 5500 psi
σhoop = PR/t = 110,000 psi
Results
Crack = 2c = 0.0133”

## Slide 4
Question 3
NASGRO
  Surface flaw = a/c = 0.5
  Geometry = SC11
    Width = 20 in
    Thickness = 0.1 in
    Diameter = 0.5
      Error occurred so changed diameter to 0.2
      This is a conservative number, lets see what happens
  Bearing load = 1000 lbs.
    = 50000 psi
  Material = Aluminum 2024-T3
    Fracture Toughness =
    Yield strength =
  Incorporate F.S. = 1.4
    KIC / 1.4
    15714

## Slide 5
Question 3 (cont)
Results
  The current flaw size in the problem is c = 0.5 in
  Is the flaw safe for flying?
    No
    Critical flaw size is 0.025
    The found flaw size is much larger than the critical crack size
  No difference in using only fracture toughness and assuming no yielding

## Slide 6
Question 4
Input
t = 0.1”
w = 0.56” (based on 2c/W < 0.5 calc)
Radiography NDE (X-ray 5009)
Proof factor = 1.5
KIC = 25000 (Al 7075-T6)
S0 = 20 ksi
Results
Operating Cycles Capability = 10511 cycles

## Slide 7: Question 5
Setup
  TC16 geometry
  Material = Al 7075-T6[12AB1]
  Airplane skin
    Flying at 40000 ft, cabin pressurized to 7000 ft
      P = 11.34 – 2.72 = 8.62 psi
      S0 = PR/t = (8.62*75)/0.1 = 6.47 ksi
    1-bay stiffened
    Radius = 75 in
    Thickness = 0.15 in
      Adjusted to 0.1 in
    Stiffener spacing = 24 in
    Rivet spacing ratio = 2/24 = 0.0833
    Dampening ratio = 0
    Biaxial load ratio = 0.5
Requirement
  3000 takeoff and landing = 3000 cycles
Assumptions
  Stiffener is made of Al 7075-T6 as well
    Elastic modulus = 10400 ksi
Units
  NASGRO material library uses the following
    Ksi for pressure
    In for length
Adjustments
  NASGRO warns of inaccuracy if thickness above 0.1 in
  Thinner wall experiences worse fatigue, should envelop original dimensions

## Slide 8: Question 5
Analysis
  3000 cycles threw error that target life is too low
  Setting more realistic target
    Using southwest as example
    Assume 3 flights/day, operating 300 days a year on average
    Quick search of airliner service life = 30 years
    3 flights = 3 cycles
      3*300 = 900 cycle/year
      900*30 = 27000 cycle/lifetime
  27000 cycle results
    C = 3.5687 in
      Round to 3.56 in
    Geometry shows that total crack length is 2c
      2*3.56 = 7.12 in
Conclusion
  3000 takeoff/landing cycle is way too little considering modern airliners
  Using quick estimate using Southwest, critical flaw size for the expected flight cycles (27000 cycles) for of an airliner is 7.12 in
    This is a conservative estimate due to reduction of thickness to avoid NASGRO inaccuracies
    With crack that big, fatigue fracture should not be the dominant failure mode for the skin
3000 cycle result
27000 cycle result

## Slide 9: Question 6
Setup
  Assume bond will fail before the metal
  We can control bond overlap length and wall thickness
    Wall thickness drives bond thickness
    Bond thickness = 0.3
    Length = overlap length
    Thickness= bond thickness
Requirement
  System must hold 400 psi internal pressure
  Fatigue not considered for problem
Assumptions
  Assume radius given is midpoint radius
  Bond material property taken from diagram
    E = 300 ksi
    V = 0.4

## Slide 10: Question 6
Analysis
  Debonding can be characterized as a crack on the bond ring
    Crack is axial, on the edge of the cylinder
  Question to ask is, at how much debonding does the bond fail?
    This length should represent minimum overlap required, assuming perfect bond
  Load on the bond can the characterized into the following
    Hoop stress experienced by the bond
    Shear experienced due to different hoop stresses between inner and outer cylinders
  Peeling stress and axial stress not considered
Test #1
  Debonding characterized as surface crack
  Based on Al 7075-T6 yield strength, we set cylinder thickness to 0.022 in
  Bond thickness = 0.3-0.022 = 0.278 in
  Bond outer diameter = 4-(0.5*0.022) = 3.989 in
  Bond hoop stress = (400*3.85)/0.278 = 5540 psi
  Inner cylinder hoop stress = (400*3.7)/0.022 = 67273 psi
  Outer cylinder hoop stress = (400*4)/0.022 = 72728 psi
  Shear caused by cylinders = 5455 psi
  Fracture toughness = K = sqrt(GE)
    Sqrt(2*300e3) = 774.59 psi-in1/2
  a/c set to maximum allowed (1.2)
    Deeper crack has higher stress concentration, which will drive catastrophic failure faster
    Gives me shortest critical flaw size
  Default units for NASGRO is Kips, in

## Slide 11: Question 6
Test #1
  Using SC04 to map bond geometry, external flaw
  Based on geometry, we can take the axial length of the critical crack size to be 2c = 2*5.294e-3 = 0.01 in
  Current understanding is that this would be the minimum overlap required to avoid failure
  Decreasing thickness of bond decreases bond’s ability to withstand fracture
    Careful balance required for Aluminum thickness
Test Result Considerations
  What critical flaw size do we say that the flaw is undetectable?
    Crack is on the edge of bond, hidden inside outer cylinder
    Most realistic NDE approach is RT or ultrasound
    Assuming we can have the same fidelity for ultrasound as the standard NDE level as shown in NASA-STD-5009
      a = 0.030 in
      a/c = 0.2
      Use these as minimum detectable flaw size
    I assumed that the standard would hold for our case due to how thin the cylinders are, and with proper test setup can achieve the same fidelity as the standard written in early 2000s
  Different approach is needed
    Try modeling bond as a plate with surface crack or through crack
    Plate can then be set with a width to specify the overlap length
    Modelled using SC02 and TC12 for each cases

## Slide 12: Question 6
Test #2
  Using SC02 for critical flaw size
  Al thickness = 0.03 in
    Slight increase to ensure both cylinders stay in elastic region with some margin
  Bond thickness = 0.27 in
  a/c = 0.2; keep with NASA STD being referenced
  Width: overlap length, variable we change to see what happens
  See image to shear modelling
    S0 represents hoop stress on the bond
    S1 represents shear stress caused by cylinders
  Bond hoop stress = (400*3.85)/0.27 = 5704 psi
  Inner cylinder hoop stress = (400*3.7)/0.03 = 49334 psi
  Outer cylinder hoop stress = (400*4)/0.03 = 53334 psi
  Shear caused by cylinders = 4000 psi
  Fracture toughness = K = sqrt(GE)
    Sqrt(2*300e3) = 774.59 psi-in1/2

## Slide 13: Question 6
Test 2 Results
  We need to find a setup where the critical flaw size is greater than what’s detectable by NASA STD NDE ultrasound
    a = 0.03 in = 3 e-2 in
    a/c = 0.2
  Keeping the a/c the same as the Standard, we approach the minimum detectable flaw size when the width = 0.5 in
  Alternative modelling using TC12 also shows that critical flaw size stays above detection range
    Through crack case examined to see if the bond itself would fail instead of delamination
Aluminum Recommendation
  Al thickness = 0.03 in
  Overlap length = 0.5 in
  Further optimization may be possible, but at current level of analysis is deemed impractical
  This will be the basis for the Abaqus setup
SC02 result (a = 3.15e-2)
TC12 result (c = 3.45e-2)

## Slide 14: Question 6
Abaqus Setup
  For the length and height of the model, we use the same one given in the image
  Changes
    Given the problem statement calls for a joint, I do not make this into a cylinder
      Assuming infinite length for the purposes of the FEA
    We add a level of conservatism since NASGRO has its limitations
      Overlap length double to 1 in
      Al thickness increased to 0.1 in
    Overlap length and thicknesses will be dimensioned for quick testing of multiple constructions
    Recall we defined the given radius as midpoint radius
  Units
    Length as in
    Force as Ibs
Material Properties
  Aluminum
    E = 10400 ksi = 10400e3 psi
    V = 0.33
  Bond
    E = 300e3 ksi = 300e6 psi
    V = 0.4
Differences between video and problem
  We don’t worry about debonding since we’re just asked to design something to survive 400 psi internal pressure
Notes regarding building model
  Using sketch to partition is much faster and less clunky than datum planes

## Slide 15: Question 6
Test #1 results
  Stress concentration at the bond edge captured
  Without debonding, Abaqus was reporting an ENRPT values of 0 across the board
  Added the following debond to capture energy release rate
    0.25 in debond from the top and the bottom, respectively
Test #1-debond results
  ENRRT max detected around the end of the debond as expected

## Slide 16: Question 6

## Slide 17: Question 6
Analysis
  G1 values for our debonded case are staying well below the bond limits
    G1c = 2
    As shown in the max value pointed in abaqus, the max G1 noticed is 2.798 e-1 on the outer layer
  This shows that our current configuration will work under 400 psi internal pressure, even with internal pressure
Additional cases to consider
  Original geometry found using NASGRO
  Replace material with steel
Original Geometry case
  Al thickness = 0.03 in
  Overlap = 0.5 in
  For debond purposes, take off ¼ of the overlap on top and bottom respectively
Steel case
  Steel material properties
    E = 30 Msi = 30e6 psi
    V = 0.3

## Slide 18: Question 6
Change Material to Steel
  G1 max = 8.859e-2
  G1 max decreased from the identical setup using Aluminum
  Stiffer material decreased the strain of the cylinders, putting less stresses on the bond

## Slide 19: Question 6
NASGRO Approach Geometry
  G1 max = 1.119
  Definite increase from the thicker geometry tested, but still under the G1c of 2

## Slide 20: Question 6
Conclusions
  NASGRO approach seems to be a valid starting point for modelling a joint for this specific case
  Caveats to FEA results
    Unlike the example images shown, I modelled this joint as connection of 2 long pipes, thus there is no top and bottom of the cylinder that would cause additional shear in the joint
    This modelling was done since it was assumed that the shear caused by the different expansion of the cylinders would be the main contributor to fracture
  Overall recommendation
    From rough understanding of fatigue fracture, the more conservative geometry is recommended for this joint
      Al thickness = 0.1 in
      Overlap = 1 in
    Switching to steel should improve fracture toughness, but this decision must be put against other factors for the joint that are not listed in the problem
      Weight margins
      Costs
      Material availability
      Fluid to be transported
    NASGRO approach does provide a rough starting point for this joint design
      However FEA is recommended for proper analysis

## Slide 21: AME 585 Fracture Project Individual Draft
1st Lt Kim, Taeklim

## Slide 22: Question 1
NASA 5019A
  Fracture control standards for human spaceflight; anything human involved comes with more stringent requirements
  1st point made regards to fracture, like all other potential failures, is setup of proper issue containment and mitigation plan
  NFC parts based on NASA testing; these are parts where other failure modes take them out before fracture
  Pressure vessels always fracture critical
  General metaling loading FOS
    4x service life factor
    1.4 FOS on single loading event
  NASGRO guidelines
    Choose Bk as zero or value so that Kc at part thickness is less than or equal to K1C
    If we need to set Bk as something else, further understanding of constraints required
  Determining flaw size using process control is unusual, need to be approved by RFCB
  flaw size determination is based on 90/95 flaw detection capability
  NDE should take the conservative estimates if unclear
    Work experience tells me NDE can be often unclear
NASA 5009
  All detected cracks, crack-like flaws to be rejected
    Accepting these flaws needs to undergo full engineering review
  NDE methods must be certified using known flaw specimens
  Standard flaw size tables provided based on shuttle test data
    Used as minimum detectable flaw siz
  Eddy current doesn’t work on composites
  Special NDE called when standard methods can’t be applied properly (complex geometry) or critical flaw size is smaller than standard flaw size
  PT, RT, ultrasound, and Eddy current for NDE
  Special NDE also needs to certify that NDE method used can achieve 90/95 flaw detection capability
  2 methods of certifying minimum detectable flaw size
    Point estimate
    POD

## Slide 23: Question 2
NASGRO Setup
  Geometry = TC07
  Use case: pipe under pressure
    Pressure = 5550 psi
    Radius = 2 in
    Thickness = 0.1 in
    Material = Al 2024-T3
  FoS = 1.4
    Apply to K1C
  Objective: find acceptable flaw size
    Need to find critical flaw size where failure occurs
    NASCCS used for this
    Fatigue not considered since we’re not solving for service life in this problem
  Al 2024-T3
    Fracture toughness (K1C) = 22e3 psi-in1/2
      Applying FOS of 1.4 = 15714 psi-in1/2
    Yield Strength = 47e3 psi
  S0 = pR/t
    (5550*1.95)/0.1
    108225 psi
  Units
    Length as in
    Force as Ibs
    Pressure as psi
    Fracture toughness as psi-in1/2

## Slide 24: Question 2
Analysis
  Overall stress induced on pipe over Al alloy yield stress, failure via yielding expected to occur before fracture
  If we are only considering the adjusted fracture toughness, then maximum acceptable flaw size is 6.642 e-3 in * 2 (flaw size is 2c)
    0.012 in max flaw size allowed

## Slide 25: Question 3
Setup
  Surface flaw = a/c = 0.5
  C = 0.5
  Geometry SC11
  Plate
    Width = 20 in
    Thickness = 0.1 in
    Hole diameter = 0.5 in
      Change diameter to 0.2 in to fit in NASGRO
      Hand calcs show smaller hole results in greater stress concentration, smaller hole should work as an enveloping case against larger hole
  S0 = 20ksi = 20e3 psi
  S3 = P/Dt
    1000/(0.5*0.1) = 20000 psi
    1000/(0.2*0.1) = 50000 psi
    Using the adjusted diameter S3 for conservatism
  Material = Al 2024-T3
    Fracture toughness (K1C) = 22e3 psi-in1/2
      Applying FOS of 1.4 = 15714 psi-in1/2
    Yield Strength = 47e3 psi
    Hand calculations show that yielding will not occur, but NASGRO limitations would artificially show yielding
      Critical flaw size will only be based on fracture toughness due to this
  Units
    Length as in
    Force as Ibs
    Pressure as psi
    Fracture toughness as psi-in1/2

## Slide 26: Question 3
Analysis
  Geometry changed to fit in NASGRO, following most conservative approach
    Hand stress calculation show that original part will not yield during operation
    Decreasing diameter is more conservative than increasing thickness in terms of preserving stress
    Decreasing the diameter results in artificial yielding in analysis, hence only using fracture toughness and forcing NASGRO to assume no yielding
  Current flaw size showing c = 0.5 in
    Bigger than critical flaw size for c = 0.025 in
  Considering the found flaw size is 20x the critical flaw size, part should be deemed unsafe for flight
    Even with the conservative adjustments made to fit in NASGRO, a 20x difference clearly indicates fracture failure occurring

## Slide 27: Question 4
Setup
  EC01 geometry
  Material = AL 7075-T6[12AB1]
    NASGRO library contains this material
  Flaw size: min detectable flaw size per NASA 5009, RT
  Testing
    Proof at 1.5 * MEOP = 30 ksi
    Leak test at 20 ksi
      Assume leak test is done at MEOP
  Thickness = 0.1 in
  Width not provided
    NASA data shows 2c = 0.14 in
    NASGRO limitation: 2c/W <= 0.5
      W >= 4c
      Fatigue fracture gets worse with smaller width
    W = 4c = 4*0.14 = 0.56 in
      We assume worst case allowed in NASGRO for conservative approach
  Cycles
    Added arbitrary service cycle to see where fatigue fracture happens
      Assumed that valve fails before 106 cycles
      Assumed that valve will cycle from ambient to MEOP
    This approach should envelop worst case scenario for valve during use

## Slide 28: Question 4
Analysis
  NASGRO predicts failure during cycle # 10511
  Valve service life is at 10000 cycles
    This does not consider operating environment, which may negatively impact service life
    This does not consider bigger flaw sizes caused in manufacturing/install/handling
  FOS considerations
    FOS should envelop human error and operating environment
    4x life usually recommended for part cycle life
  Adjusted valve service life
    10000/4 = 2500
    Adjusted service life recommendation = 2500 cycles

## Slide 29: Question 5
Setup
  TC16 geometry
  Material = Al 7075-T6[12AB1]
  Airplane skin
    Flying at 40000 ft, cabin pressurized to 7000 ft
      P = 11.34 – 2.72 = 8.62 psi
      S0 = PR/t = (8.62*75)/0.1 = 6.47 ksi
    1-bay stiffened
    Radius = 75 in
    Thickness = 0.15 in
      Adjusted to 0.1 in
    Stiffener spacing = 24 in
    Rivet spacing ratio = 2/24 = 0.0833
    Dampening ratio = 0
    Biaxial load ratio = 0.5
Requirement
  3000 takeoff and landing = 3000 cycles
Assumptions
  Stiffener is made of Al 7075-T6 as well
    Elastic modulus = 10400 ksi
Units
  NASGRO material library uses the following
    Ksi for pressure
    In for length
Adjustments
  NASGRO warns of inaccuracy if thickness above 0.1 in
  Thinner wall experiences worse fatigue, should envelop original dimensions

## Slide 30: Question 5
Analysis
  3000 cycles threw error that target life is too low
  Setting more realistic target
    Using southwest as example
    Assume 3 flights/day, operating 300 days a year on average
    Quick search of airliner service life = 30 years
    3 flights = 3 cycles
      3*300 = 900 cycle/year
      900*30 = 27000 cycle/lifetime
  27000 cycle results
    C = 3.5687 in
      Round to 3.56 in
    Geometry shows that total crack length is 2c
      2*3.56 = 7.12 in
Conclusion
  3000 takeoff/landing cycle is way too little considering modern airliners
  Using quick estimate using Southwest, critical flaw size for the expected flight cycles (27000 cycles) for of an airliner is 7.12 in
    This is a conservative estimate due to reduction of thickness to avoid NASGRO inaccuracies
    With crack that big, fatigue fracture should not be the dominant failure mode for the skin
3000 cycle result
27000 cycle result

## Slide 31: Question 6
Setup
  Assume bond will fail before the metal
  We can control bond overlap length and wall thickness
    Wall thickness drives bond thickness
    Bond thickness = 0.3
    Length = overlap length
    Thickness= bond thickness
Requirement
  System must hold 400 psi internal pressure
  Fatigue not considered for problem
Assumptions
  Assume radius given is midpoint radius
  Bond material property taken from diagram
    E = 300 ksi
    V = 0.4

## Slide 32: Question 6
Analysis
  Debonding can be characterized as a crack on the bond ring
    Crack is axial, on the edge of the cylinder
  Question to ask is, at how much debonding does the bond fail?
    This length should represent minimum overlap required, assuming perfect bond
  Load on the bond can the characterized into the following
    Hoop stress experienced by the bond
    Shear experienced due to different hoop stresses between inner and outer cylinders
  Peeling stress and axial stress not considered
Test #1
  Debonding characterized as surface crack
  Based on Al 7075-T6 yield strength, we set cylinder thickness to 0.022 in
  Bond thickness = 0.3-0.022 = 0.278 in
  Bond outer diameter = 4-(0.5*0.022) = 3.989 in
  Bond hoop stress = (400*3.85)/0.278 = 5540 psi
  Inner cylinder hoop stress = (400*3.7)/0.022 = 67273 psi
  Outer cylinder hoop stress = (400*4)/0.022 = 72728 psi
  Shear caused by cylinders = 5455 psi
  Fracture toughness = K = sqrt(GE)
    Sqrt(2*300e3) = 774.59 psi-in1/2
  a/c set to maximum allowed (1.2)
    Deeper crack has higher stress concentration, which will drive catastrophic failure faster
    Gives me shortest critical flaw size
  Default units for NASGRO is Kips, in

## Slide 33: Question 6
Test #1
  Using SC04 to map bond geometry, external flaw
  Based on geometry, we can take the axial length of the critical crack size to be 2c = 2*5.294e-3 = 0.01 in
  Current understanding is that this would be the minimum overlap required to avoid failure
  Decreasing thickness of bond decreases bond’s ability to withstand fracture
    Careful balance required for Aluminum thickness
Test Result Considerations
  What critical flaw size do we say that the flaw is undetectable?
    Crack is on the edge of bond, hidden inside outer cylinder
    Most realistic NDE approach is RT or ultrasound
    Assuming we can have the same fidelity for ultrasound as the standard NDE level as shown in NASA-STD-5009
      a = 0.030 in
      a/c = 0.2
      Use these as minimum detectable flaw size
    I assumed that the standard would hold for our case due to how thin the cylinders are, and with proper test setup can achieve the same fidelity as the standard written in early 2000s
  Different approach is needed
    Try modeling bond as a plate with surface crack or through crack
    Plate can then be set with a width to specify the overlap length
    Modelled using SC02 and TC12 for each cases

## Slide 34: Question 6
Test #2
  Using SC02 for critical flaw size
  Al thickness = 0.03 in
    Slight increase to ensure both cylinders stay in elastic region with some margin
  Bond thickness = 0.27 in
  a/c = 0.2; keep with NASA STD being referenced
  Width: overlap length, variable we change to see what happens
  See image to shear modelling
    S0 represents hoop stress on the bond
    S1 represents shear stress caused by cylinders
  Bond hoop stress = (400*3.85)/0.27 = 5704 psi
  Inner cylinder hoop stress = (400*3.7)/0.03 = 49334 psi
  Outer cylinder hoop stress = (400*4)/0.03 = 53334 psi
  Shear caused by cylinders = 4000 psi
  Fracture toughness = K = sqrt(GE)
    Sqrt(2*300e3) = 774.59 psi-in1/2

## Slide 35: Question 6
Test 2 Results
  We need to find a setup where the critical flaw size is greater than what’s detectable by NASA STD NDE ultrasound
    a = 0.03 in = 3 e-2 in
    a/c = 0.2
  Keeping the a/c the same as the Standard, we approach the minimum detectable flaw size when the width = 0.5 in
  Alternative modelling using TC12 also shows that critical flaw size stays above detection range
    Through crack case examined to see if the bond itself would fail instead of delamination
Aluminum Recommendation
  Al thickness = 0.03 in
  Overlap length = 0.5 in
  Further optimization may be possible, but at current level of analysis is deemed impractical
  This will be the basis for the Abaqus setup
SC02 result (a = 3.15e-2)
TC12 result (c = 3.45e-2)

## Slide 36: Question 6
Abaqus Setup
  For the length and height of the model, we use the same one given in the image
  Changes
    Given the problem statement calls for a joint, I do not make this into a cylinder
      Assuming infinite length for the purposes of the FEA
    We add a level of conservatism since NASGRO has its limitations
      Overlap length double to 1 in
      Al thickness increased to 0.1 in
    Overlap length and thicknesses will be dimensioned for quick testing of multiple constructions
    Recall we defined the given radius as midpoint radius
  Units
    Length as in
    Force as Ibs
Material Properties
  Aluminum
    E = 10400 ksi = 10400e3 psi
    V = 0.33
  Bond
    E = 300e3 ksi = 300e6 psi
    V = 0.4
Differences between video and problem
  We don’t worry about debonding since we’re just asked to design something to survive 400 psi internal pressure
Notes regarding building model
  Using sketch to partition is much faster and less clunky than datum planes

## Slide 37: Question 6
Test #1 results
  Stress concentration at the bond edge captured
  Without debonding, Abaqus was reporting an ENRPT values of 0 across the board
  Added the following debond to capture energy release rate
    0.25 in debond from the top and the bottom, respectively
Test #1-debond results
  ENRRT max detected around the end of the debond as expected

## Slide 38: Question 6

## Slide 39: Question 6
Analysis
  G1 values for our debonded case are staying well below the bond limits
    G1c = 2
    As shown in the max value pointed in abaqus, the max G1 noticed is 2.798 e-1 on the outer layer
  This shows that our current configuration will work under 400 psi internal pressure, even with internal pressure
Additional cases to consider
  Original geometry found using NASGRO
  Replace material with steel
Original Geometry case
  Al thickness = 0.03 in
  Overlap = 0.5 in
  For debond purposes, take off ¼ of the overlap on top and bottom respectively
Steel case
  Steel material properties
    E = 30 Msi = 30e6 psi
    V = 0.3

## Slide 40: Question 6
Change Material to Steel
  G1 max = 8.859e-2
  G1 max decreased from the identical setup using Aluminum
  Stiffer material decreased the strain of the cylinders, putting less stresses on the bond

## Slide 41: Question 6
NASGRO Approach Geometry
  G1 max = 1.119
  Definite increase from the thicker geometry tested, but still under the G1c of 2

## Slide 42: Question 6
Conclusions
  NASGRO approach seems to be a valid starting point for modelling a joint for this specific case
  Caveats to FEA results
    Unlike the example images shown, I modelled this joint as connection of 2 long pipes, thus there is no top and bottom of the cylinder that would cause additional shear in the joint
    This modelling was done since it was assumed that the shear caused by the different expansion of the cylinders would be the main contributor to fracture
  Overall recommendation
    From rough understanding of fatigue fracture, the more conservative geometry is recommended for this joint
      Al thickness = 0.1 in
      Overlap = 1 in
    Switching to steel should improve fracture toughness, but this decision must be put against other factors for the joint that are not listed in the problem
      Weight margins
      Costs
      Material availability
      Fluid to be transported
    NASGRO approach does provide a rough starting point for this joint design
      However FEA is recommended for proper analysis

## Slide 43: AME 585 Project 7
Samy Ousman

## Slide 44
Question 1
NASA 5019A
Develop a Comprehensive Fracture Control Plan (FCP): Establishing and maintaining an FCP is crucial for human-rated spaceflight hardware to mitigate catastrophic failure risks due to flaws.
Classify Hardware Components Accurately: All parts should be evaluated and categorized as exempt, non-fracture critical (NFC), or fracture critical to determine appropriate control measures.
Implement Rigorous Verification Processes: Verification of fracture control requirements ensures that hardware meets safety and reliability standards.
Utilize Established Approaches for Specific Hardware Types: Applying proven methods for different hardware categories enhances reliability and safety.
Document Alternative Approaches Thoroughly: When deviating from standard practices, comprehensive documentation and approval are essential to maintain safety standards.
Ensure Material Traceability: Maintaining traceability of materials used in fracture-critical components is vital for quality assurance and safety.
Perform Detailed Failure Mode Evaluations: Identifying and assessing potential failure modes in hardware components help in implementing effective fracture control measures.
Apply Conservative Design Margins: Incorporating conservative design margins in fracture-critical components enhances safety and reliability.
Conduct Regular Training for Personnel: Ensuring that personnel involved in fracture control are adequately trained contributes to the effectiveness of the program.
Engage in Continuous Improvement: Regularly updating fracture control practices based on new findings and technological advancements fosters ongoing enhancement of safety measures.
NASA 5009
Establish Clear NDE Requirements: Defining specific NDE requirements for fracture-critical components ensures consistent application across programs.
Qualify NDE Procedures Rigorously: Qualification of NDE procedures is essential to validate their effectiveness in detecting critical flaws.
Determine Minimum Detectable Flaw Sizes: Establishing the smallest flaw size that NDE methods can reliably detect is crucial for accurate fracture analysis.
Apply Standard NDE Methods When Appropriate: Utilizing standard NDE methods with known capabilities simplifies the inspection process and ensures reliability.
Implement Special NDE for Complex Cases: For unique or complex components, special NDE procedures may be necessary to achieve the required detection capabilities.
Maintain Inspector Proficiency: Regular training and certification of NDE inspectors are vital to maintain high detection reliability.
Document NDE Results Systematically: Thorough documentation of NDE findings supports traceability and aids in the assessment of component integrity.
Integrate NDE into the Design Process: Incorporating NDE considerations early in the design phase facilitates the development of inspectable and reliable components.
Utilize Probability of Detection (POD) Curves: Employing POD curves helps in understanding the effectiveness of NDE methods and informs risk assessments.
Engage in Continuous NDE Technology Assessment: Regularly evaluating and adopting advancements in NDE technologies ensures the effectiveness of inspection processes.

## Slide 45
Question 2
Input
R = 2”; D = 4”
t = 0.1”
KIC = 22000 (Al 2024-T3)
FS = 1.4
KIC = 22000/1.4 = 15714
P = 5500 psi
σhoop = PR/t = 110,000 psi
Results
Crack = 2c = 0.0133”

## Slide 46
Question 3
NDE
a/c = 0.5 (c = 0.5”)
a = 0.25” acceptable?
Input
t = 0.1”
w = 20”
D = .2” (0.5 < D/t <2)
a/c = 0.5
KIC = 22000 (Al 2024-T3)
P = 5500 psi
S0 = 20 ksi
P = 1000 lb
S3 = P/Dt = 20 ksi
Results
Critical Crack Size = c = 0.1” > 0.5”
Unsafe for flight conditions

## Slide 47
Question 4
Input
t = 0.1”
w = 0.56” (based on 2c/W < 0.5 calc)
Radiography NDE (X-ray 5009)
Proof factor = 1.5
KIC = 25000 (Al 7075-T6)
S0 = 20 ksi
Results
Operating Cycles Capability = 10511 cycles

## Slide 48
Question 5
Input
S0 = PR/t = (8.62*75)/.1 = 6.47 ksi
KIC = 25000 (Al 7075-T6)
E = 10400 ksi
Results
Critical Crack Size = 2c = 24.03” (anything above this value will decrease capability below 300 cycles)

## Slide 49
Question 6
From NASGRO
t = 0.27”

## Slide 50
Question 6: Aluminum 7075-T6
Results (No Bonding)
Stress = 32.1 ksi
ENPRT = 0

## Slide 51
Question 6: Aluminum 7075-T6
Results (Debond)
Stress = 32.1 ksi
ENPRT = 5.23E-2

## Slide 52
Question 6: Steel
Results (Debond)
Stress = 29.8 ksi
ENPRT = 4.5E3

## Slide 53
AME 585
Project 7
Henry Glover
3/14/2025

## Slide 54
#1
NASA 5019
  A fracture control plan needs to be developed and maintained for human rated spaceflight hardware that
    Addresses hazard, the parts in the program-specific flight hardware
    Meets the requirements of the NASA technical slandered
    Specifics fracture controls to mitigate risk of catastrophic failure
    Has approval by the RFCB
  If part failure does not result in a credible catastrophic hazard, then it is classified as non-fracture critical
  For pressurized components perform proof tests to a minimum of 1.5 times the MDP during individual acceptance
  For rotating hardware, it is proofed by a spin test to a minimum rotational energy factor of 1.05
  A loading spectra is needed for the damager tolerance life analysis
  Assume that initial flaw in a part is the size and shape that is not screened by NDE, proof test, or process control and it is in the worst location and orientation
  If fatigue crack growth is minimal or the service life is a single event, the analysis must ensure a factor of safety of 1.4 on the critical stress intensity factor
  Develop an impact damage mitigation plan to define, document, implement, and prescribe impact protection and detection strategies for flight hardware to mitigate identified damage threats
  For proof testing composite or bonded hardware a flight article needs to be 1.2 times the limit load under the appropriate environment conditions or by adjusting the test loads using coupon or hardware element tests verified ECF
  All parts go through a fracture control classification process for all mission phases to determine which parts are fracture critical. Parts are classified as:
    Exempt
    NFC – Not fracture critical
    Fracture critical

## Slide 55
#1 Cont.
NASA 5009
  NDE inspection is conducted by certified inspectors who have a clear criteria defined for each type of part and NDE methods need to be selected for the entirety of the component's life cycles including – manufacturing, transportation, maintance, and operations
  All detected crack or crack-like flaws can be cause for rejection
  NDE inspection zones need to be clearly identified in drawings and subsequently updated
  NDE capability demonstration specimens must be used to assess detection capability for Special NDE applications, represent the inspected material and flaw characteristics, and be documented in NDE procedures and personnel qualifications, with specimens sourced or created as needed
  Nondestructive inspections of fracture-critical hardware must detect initial crack sizes from damage tolerance analyses with 90% probability at 95% confidence
  Liquid penetrant testing (fluorescent penetrant), eddy current, magnetic particle inspections, UT, RT, and other NDE need to be in accordance with the standard practices and specification sheets (ASTM, SAE, etc.)
  All deviations from the standard NDE need to be approved by the qualified and approved NDE engineering organization, the RFCB, and the Technical Authority
  Special NDE is require with approval when the damage tolerance analysis requires smaller flaw sizes than those given for standard NDE
  The Point Estimate Method assumes flaw detection capability increases with flaw size near the test flaw and requires few flaws, making the minimum detectable flaw size potentially non-determinant
  NDE needs a summary report with the supporting data

## Slide 56
#2
NASGRO
  Geometry = TC07
    Radius = 2 in
    Diameter = 2 x R = 4
    Thickness = 0.1 in
  Material = Aluminum 2024-T3
    Fracture Toughness =
    Yield strength =
  Through crack in a pipe
    Crack propagation analysis
    NASCCS
  Pressure = 5,550 psi
  Incorporate F.S. = 1.4
    KIC / 1.4
    15714
  = 1.95
  108225 psi
  Is the acceptable flaw size inspectable by dye penetrant?
    Need to find critical crack size
Aluminum Properties - https://www.makeitfrom.com/material-properties/2024-T3-Aluminum

## Slide 57
#2 Cont..
Results
  Max acceptable flaw size =
    0.0067
    2C = 0.0134 in
  This was calculated using an outer diameter of 4 in.

## Slide 58
Question 3
NASGRO
  Surface flaw = a/c = 0.5
  Geometry = SC11
    Width = 20 in
    Thickness = 0.1 in
    Diameter = 0.5
      Error occurred so changed diameter to 0.2
      This is a conservative number, lets see what happens
  Bearing load = 1000 lbs.
    = 50000 psi
  Material = Aluminum 2024-T3
    Fracture Toughness =
    Yield strength =
  Incorporate F.S. = 1.4
    KIC / 1.4
    15714

## Slide 59
Question 3 (cont)
Results
  The current flaw size in the problem is c = 0.5 in
  Is the flaw safe for flying?
    No
    Critical flaw size is 0.025
    The found flaw size is much larger than the critical crack size
  No difference in using only fracture toughness and assuming no yielding

## Slide 60
#4
AL 7075-T6 [12AB1]
Thickness = 0.1 in
Width
  2c/W <= 0.5
  c = 0.07
  2c = 0.14
  W >= 4c
  W = 0.56
Pressure = 20 Ksi
Use X-ray 5009 flaw size
Assumptions
  EC01 is the right geometry
  Proof factor = 1.5
    30 Ksi
  Proof test completed once
Leak test at 20 Ksi
Cycles set to infinity to see when the valve will fail

## Slide 61
#4 Cont.
Results
  Failure at cycle 10511
  Based on FOS of 4x, valve service life should be at 2500 cycles
  This doesn’t not account for temperature fluctuations, manufacturing variability, handling, or environmental loads on the valve

## Slide 62
#5
TC16
Assumptions
  Flying at = 40,000 ft
  Cabin pressure = 7,000 ft
  P = 11.34 - 2.72 = 8.62 psi
  S0 = PR/t = 6.47
Al 7075-T6[12AB1]
  E = 10400
1-bay stiffened
  Area =1 in2
  Rivet every 2 in
  Length between stiffeners = 24 in
Radius = 75 in
Thickness = 0.15
  NASGRO adjusted to 0.1 thickness
Biaxial load ratio = 0.5
Dampening ratio = 0

## Slide 63
#5 Cont.
Results
  Iterate crack size, until a finite life solution
  3.35 crack size
  2 x 3.35 = 6.7 in
  Conservative estimate of 6.7 in of a critical crack size

## Slide 64
#6
Tubular joint under pressure
Fracture toughness = 2 lb/in
Aluminum 7075
Cannot rupture at an internal pressure of 400 Psi
Bond thickness = 0.27
Bond hoop stress = (400*3.85)/0.27 = 5704 psi​
Inner cylinder hoop stress = (400*3.7)/0.03 = 49334 psi​
Outer cylinder hoop stress = (400*4)/0.03 = 53334 psi​
Shear caused by cylinders = 4000 psi​
Fracture toughness = K = sqrt(GE)​
Sqrt(2*300e3) = 774.59 psi-in1/2​

## Slide 65
#6 Cont.
Results using SC02
  a = 3.8157e-3

## Slide 66
#6 Cont.
Abaqus setup
  Joint thickness = 0.25
  Upper and lower bounds were kept the same from the video
  Partitions were created to discretize mesh

## Slide 67
#6 Cont.
Mesh was changed to structures
Mesh seeds were set

## Slide 68
#6 Cont.
Load of 250 Psi was placed
Mesh for the joint was set

## Slide 69
#6 Cont.
Result with no debonding showed 0 ENRPT11
Deformation was located on the y-constraint

## Slide 70
#6 Cont.
To add debonding, the structure was altered

## Slide 71
#6 Cont.
Aluminum structure with debonding

## Slide 72
#6 Cont.
Steel structure with debonding