## Slide 1
AME 585
Project 7
Henry Glover
3/14/2025

## Slide 2
#1
NASA 5019
  A fracture control plan needs to be developed and maintained for human rated spaceflight hardware that
    Addresses hazard, the parts in the program-specific flight hardware
    Meets the requirements of the NASA technical slandered
    Specifics fracture controls to mitigate risk of catastrophic failure
    Has approval by the RFCB
  If part failure does not result in a credible catastrophic hazard, then it is classified as non-fracture critical
  For pressurized components perform proof tests to a minimum of 1.5 times the MDP during individual acceptance
  For rotating hardware, it is proofed by a spin test to a minimum rotational energy factor of 1.05
  A loading spectra is needed for the damager tolerance life analysis
  Assume that initial flaw in a part is the size and shape that is not screened by NDE, proof test, or process control and it is in the worst location and orientation
  If fatigue crack growth is minimal or the service life is a single event, the analysis must ensure a factor of safety of 1.4 on the critical stress intensity factor
  Develop an impact damage mitigation plan to define, document, implement, and prescribe impact protection and detection strategies for flight hardware to mitigate identified damage threats
  For proof testing composite or bonded hardware a flight article needs to be 1.2 times the limit load under the appropriate environment conditions or by adjusting the test loads using coupon or hardware element tests verified ECF
  All parts go through a fracture control classification process for all mission phases to determine which parts are fracture critical. Parts are classified as:
    Exempt
    NFC – Not fracture critical
    Fracture critical

## Slide 3
#1 Cont.
NASA 5009
  NDE inspection is conducted by certified inspectors who have a clear criteria defined for each type of part and NDE methods need to be selected for the entirety of the component's life cycles including – manufacturing, transportation, maintance, and operations
  All detected crack or crack-like flaws can be cause for rejection
  NDE inspection zones need to be clearly identified in drawings and subsequently updated
  NDE capability demonstration specimens must be used to assess detection capability for Special NDE applications, represent the inspected material and flaw characteristics, and be documented in NDE procedures and personnel qualifications, with specimens sourced or created as needed
  Nondestructive inspections of fracture-critical hardware must detect initial crack sizes from damage tolerance analyses with 90% probability at 95% confidence
  Liquid penetrant testing (fluorescent penetrant), eddy current, magnetic particle inspections, UT, RT, and other NDE need to be in accordance with the standard practices and specification sheets (ASTM, SAE, etc.)
  All deviations from the standard NDE need to be approved by the qualified and approved NDE engineering organization, the RFCB, and the Technical Authority
  Special NDE is require with approval when the damage tolerance analysis requires smaller flaw sizes than those given for standard NDE
  The Point Estimate Method assumes flaw detection capability increases with flaw size near the test flaw and requires few flaws, making the minimum detectable flaw size potentially non-determinant
  NDE needs a summary report with the supporting data

## Slide 4
#2
NASGRO
  Geometry = TC07
    Radius = 2 in
    Diameter = 2 x R = 4
    Thickness = 0.1 in
  Material = Aluminum 2024-T3
    Fracture Toughness =
    Yield strength =
  Through crack in a pipe
    Crack propagation analysis
    NASCCS
  Pressure = 5,550 psi
  Incorporate F.S. = 1.4
    KIC / 1.4
    15714
  = 1.95
  108225 psi
  Is the acceptable flaw size inspectable by dye penetrant?
    Need to find critical crack size
Aluminum Properties - https://www.makeitfrom.com/material-properties/2024-T3-Aluminum

## Slide 5
#2 Cont..
Results
  Max acceptable flaw size =
    0.0067
    2C = 0.0134 in
  This was calculated using an outer diameter of 4 in.

## Slide 6
#3
NASGRO
  Surface flaw = a/c = 0.5
  Geometry = SC11
    Width = 20 in
    Thickness = 0.1 in
    Diameter = 0.5
      Error occurred so changed diameter to 0.2
      This is a conservative number, lets see what happens
  Bearing load = 1000 lbs.
    = 50000 psi
  Material = Aluminum 2024-T3
    Fracture Toughness =
    Yield strength =
  Incorporate F.S. = 1.4
    KIC / 1.4
    15714

## Slide 7
#3 Cont.
Results
  The current flaw size in the problem is c = 0.5 in
  Is the flaw safe for flying?
    No
    Critical flaw size is 0.025
    The found flaw size is much larger than the critical crack size
  No difference in using only fracture toughness and assuming no yielding

## Slide 8
#4
AL 7075-T6 [12AB1]
Thickness = 0.1 in
Width
  2c/W <= 0.5
  c = 0.07
  2c = 0.14
  W >= 4c
  W = 0.56
Pressure = 20 Ksi
Use X-ray 5009 flaw size
Assumptions
  EC01 is the right geometry
  Proof factor = 1.5
    30 Ksi
  Proof test completed once
Leak test at 20 Ksi
Cycles set to infinity to see when the valve will fail

## Slide 9
#4 Cont.
Results
  Failure at cycle 10511
  Based on FOS of 4x, valve service life should be at 2500 cycles
  This doesn’t not account for temperature fluctuations, manufacturing variability, handling, or environmental loads on the valve

## Slide 10
#5
TC16
Assumptions
  Flying at = 40,000 ft
  Cabin pressure = 7,000 ft
  P = 11.34 - 2.72 = 8.62 psi
  S0 = PR/t = 6.47
Al 7075-T6[12AB1]
  E = 10400
1-bay stiffened
  Area =1 in2
  Rivet every 2 in
  Length between stiffeners = 24 in
Radius = 75 in
Thickness = 0.15
  NASGRO adjusted to 0.1 thickness
Biaxial load ratio = 0.5
Dampening ratio = 0

## Slide 11
#5 Cont.
Results
  Iterate crack size, until a finite life solution
  3.35 crack size
  2 x 3.35 = 6.7 in
  Conservative estimate of 6.7 in of a critical crack size

## Slide 12
#6
Tubular joint under pressure
Fracture toughness = 2 lb/in
Aluminum 7075
Cannot rupture at an internal pressure of 400 Psi
Bond thickness = 0.27
Bond hoop stress = (400*3.85)/0.27 = 5704 psi​
Inner cylinder hoop stress = (400*3.7)/0.03 = 49334 psi​
Outer cylinder hoop stress = (400*4)/0.03 = 53334 psi​
Shear caused by cylinders = 4000 psi​
Fracture toughness = K = sqrt(GE)​
Sqrt(2*300e3) = 774.59 psi-in1/2​

## Slide 13
#6 Cont.
Results using SC02
  a = 3.8157e-3

## Slide 14
#6 Cont.
Abaqus setup
  Joint thickness = 0.25
  Upper and lower bounds were kept the same from the video
  Partitions were created to discretize mesh

## Slide 15
#6 Cont.
Mesh was changed to structures
Mesh seeds were set

## Slide 16
#6 Cont.
Load of 250 Psi was placed
Mesh for the joint was set

## Slide 17
#6 Cont.
Result with no debonding showed 0 ENRPT11
Deformation was located on the y-constraint

## Slide 18
#6 Cont.
To add debonding, the structure was altered

## Slide 19
#6 Cont.
Aluminum structure with debonding

## Slide 20
#6 Cont.
Steel structure with debonding