## Slide 1
AME 585
Project 8
Henry Glover
3/27/2025

## Slide 2
#1
Why failure occurs when air is entrapped in a honeycomb
  Generates a differential pressure across the face-sheets during ascent
    Due to external atmospheric pressure decreasing as altitude increases
    Due to trapped air expanding from aerodynamic heating (may exceed >20 Psi of pressure)
  Internal cavity pressure accompanies an unvented core
    Adhesive failures due to weak face-sheet core bondlines
    Face-sheet separation or rupture
  Compression loads can further expand the effects of pressure differential
  Change is pressure is the main cause of failure in an unvented core
Defects are not necessary to enable this failure mode
  Defects can activate/inhibit catastrophic failure
    Decreases the structures' ability to resist negative effects/failure’s
  Poor manufacturing quality issues can affect bondline strength
  Aging of adhesive, poor surface preparation, contamination, cure cycle problems, uniformity of cure pressure, improper dry fit, improper storage

## Slide 3
#2
Moisture
  In an unvented honeycomb, moisture or entrapped air cannot escape causing internal, unwanted pressure within the structure
  During harsh launch conditions or environments, the moisture can be heated and turned into gasses that can creates additional internal pressure
    Moisture can also freeze are create unwanted problems
    Can also cause a corrosive environment that can be a determent to the mechanical properties, reducing strength and life of the component
  Need to avoid moisture absorbing core materials
Heat
  Heat can cause air to expand, leading to over pressurization and pressure build up
    Can cause debonding/delamination
Overtime, the cycle pressurization and in-plane loading can affect disbanding propagation and structural integrity

## Slide 4
#3
Energy release rate
  Amount of energy released per unit area of crack growth in a material
  Amount of stored elastic energy to drive the propagation of a crack in a composite structure
    Interface between face-sheet and core
Fracture toughness is the critical energy release rate
  Threshold value of energy release rate at which a crack begins to propagate
  If applied energy release rates exceed the critical energy release rate, the crack will grow
Single Cantilever beam (SCB) test
  Used to measure fracture toughness in composite structures
  It specifically tests, Mode 1 loading (opening)
  How it works
    A specimen with pre delamination is bonded on one side
    The cantilever is loaded on the free end of the specimen causing the crack to open and propagate
    Load and displacements are measured
    The energy release rates are found using beam theory as the crack propagates
  Useful for characterizing the face-sheet and core interface in composite structures
https://www.researchgate.net/figure/Single-cantilever-beam-Mode-1-fracture-test-SCB-configuration_fig1_358431799
https://www.compositesworld.com/articles/the-single-cantilever-beam-test-for-sandwich-composites

## Slide 5
#4
3 aircraft incidents due to unvented honeycomb designs
Air Transat Flight 961 – Airbus A310 - 308 aircraft
  At cruising altitude, the rudder fell off and the aircraft entered a Dutch roll
  Pilots were able to stabilize aircraft and return safely
  Rudder is a sandwich composite constructed of a non-metallic Nomex® aramid-based honeycomb core, with CFRP face-sheets, and a glass fiber-reinforced plastic (GFRP) intermediate layer between the CFRP and the honeycomb
  There is a layer of Tedlar® on the interior face for moisture protection, and a layer of film adhesive (AF 126) on the exterior face for aerodynamic smoothness
  Pieces of honeycomb are bonded together along their side edges by a bonding adhesive and unvented for aerodynamic purposes
  Findings concluded that the rudder had pre-existing dis-bond or an in-plane core fracture that deteriorate in flight
    Caused by poor manufacture’s recommended inspection policy that was not adequate in detecting all rudder defects
https://journals.sagepub.com/doi/full/10.1177/10996362221116887
https://www.tsb.gc.ca/eng/rapports-reports/aviation/2005/a05f0047/a05f0047.html

## Slide 6
#4 Cont.
3 aircraft incidents due to unvented honeycomb designs
  RAAF F-111 aircraft
    Made up honeycomb sandwich panels
    Serious degradation issues that cause failure
    Panels were found on the aircraft with large areas of adhesive bond separation and corrosion damage
    Damage was caused by the ingress of water in the panels either because of poor sealing from the manufacture or after a failed repair
    Moisture in the panel caused adhesive degradation that reduced material strength on the bonds holding the panels together
  Boeing 747-433 (Cargo)
    In 2024, an upper left-wing panel detached from the aircraft during landing
    Caused by fatigue cracking in the honeycomb structure
    FOD on the runway was of main concern as the wind panel detachment had minimal impact on controllability
    Manufacture released a service bulletin but it did little to prevent the incident
https://apps.dtic.mil/sti/tr/pdf/ADA385139.pdf
https://en.wikipedia.org/wiki/General_Dynamics_F-111C

## Slide 7
#4 Cont.
3 spacecraft incidents due to unvented honeycomb designs
  Block II Global Positioning System
    Initially used an unvented honeycomb design to avoid outgassing in the Space Shuttle cargo bay
    Testing revealed the bond failed during thermal cycling
    Panel rupture occurred at the thinner skin without Kapton during testing, so in 1983 the engineers switched to a vented honeycomb core and a higher temp FM-300 adhesive
  X-33 LH2 Tank Failure
    Unvented honeycomb design with graphite epoxy facesheets
    LH2 tank failed during testing due to pressure buildup in the core of the sandwich
    Fachseets disbanded and separated from the core
    Caused by microcracking, hydrogen pressure buildup, manufacture flaws, and reduced bondline strength
  Loral space systems
    Experienced solar array damage
    Caused by a tight seal at the end of the solar panels that prevented necessary venting and proper bonding
    Pressure build up in the honeycomb structure that caused an explosive depressurization
    Caused by manufacturing defects and flaws
https://apps.dtic.mil/sti/pdfs/ADA276713.pdf
https://ntrs.nasa.gov/api/citations/20030067586/downloads/20030067586.pdf
https://journals.sagepub.com/doi/full/10.1177/10996362221116887
https://www.spacesafetymagazine.com/aerospace-engineering/spacecraft-design/space-systemsloral-case-study-ineffective-incident-investigation/

## Slide 8
#4 Cont.
3 launch vehicle incidents due to unvented honeycomb designs
  Titan III LV in 1966
    Fiberglass honeycomb sandwich payload fairing exploded
    Investigation showed that the stresses induced by aerodynamic heating were relatively low, but the lack of venting and defects lead to failure
    Improved skin-to-core bonding, better testing methods (for the time), denser honeycomb cores, and process to reduce water absorption
  Atlas AC-58 payload fairing
    In 1987 a proof test of the AC-58 payload fairing failed due to inner skin-to-core disbanding
    Failure originated from a weak bond area undetected by NDE “tap” testing
      The flaw was possibly caused by contamination, poor adhesive flow, or low cure pressure/temp
    Non-veneted honeycomb construction also affected AC-59 payload fairing
  Mariner 3
    Mars probe that was commissioned to take pictures of mars in 1964
    Failed due to the shrouds inner fiberglass separating from the shrouds outer skin, preventing jettison
      Was a pressure buildup in the fiberglass honeycomb core
      Ground tests were never conducted with the combined pressure and temperature environment
https://apps.dtic.mil/sti/pdfs/ADA276713.pdf

## Slide 9
#5
Acceptance testing performed on spacecraft and aircraft
  Weak bonds between the core and the face-sheet can be hard to detect using standard NDE methods
  Finding the acceptable flaw size is instrumental in proof testing
    Load definition
      External loads
      Core pressure
        Venting rates
        Heating environments
        Altitude
    Building block approach
      Face-sheet failure strength
      Find core-to-facesheet interfacial fracture toughness
      Environmental strength reduction
      Combined load testing (pressure + external loads)
    Define acceptable flaw size
  Develop NDE that can detect flaw size
    Hand-held ultrasonic inspection
    Shearography
    Flash thermography
    Pulse echo ultrasound
    Air-coupled through transmission
Proof test to match requirements
Pre and post proof NDE to demonstrate flaw within envelope

## Slide 10
#6
“We have flown successfully before”
  Complacency and comfort is detrimental to any industry
    Have to cross your T’s and dot your I’s
  Just because a system has prior success it still must undergo a rigorous verification process
  Verification, redesign, proof testing, inspection are among the few things that need to occur before recommissioning a structure or using old information
  Have to treat every mission with the same standards and same level of importance
  In every flight and every design there are new challenges, new failures, and new information that may have not been available before
  Just because it works once, twice….etc. doesn’t mean it will automatically work every time
    This is a boost of confidence for a system but does not substitute verification

## Slide 11
#7
Biggest lesson learned
  Unvented honeycombs have their place in Aerospace
    Used for aerodynamic purposes
    Needs constant inspection and maintenance schedules
    Corrosion is less likely to happen because they are sealed
  Vented honeycombs have their place in Aerospace as well
    No air entrapment – no pressure build up
    No moisture build up
    Corrosion susceptible
    Good thermal properties
    Vented honeycombs used in space application on LV and Spacecraft
  That being said, both have their pros and cons
  Both are susceptible to manufacturing and handling defects
  A vented design can act like an unvented design if it is manufactured incorrectly
    Venting rates can be so poor or improperly manufactured that they are basically useless and act like unvented honeycombed composites

## Slide 12
#8
10 lessons learned - https://ntrs.nasa.gov/citations/20090008664
  The use of finite element thermal solver is very important for ascent rate heating and honeycomb composite understanding
  Result comparison using different FEA software's is important for redundancy
  The use of a temperature-based heat transfer coefficient increased supposed results
  Heating rates provided in the data include gas convection, gas radiation, particle convection, and particle kinetic energy heat transfer
  For the spacecraft adapter (SA) only gas convection contributes to heating rate
  Spacecraft adaptors (SA) fairings are formed by a honeycomb core and an inner face sheet
  Necessary thermal protection is need for areas where the temperature can reach higher than predicted
  The ascent trajectory and profile significantly influence the thermal environment and need to be considered
  Collaboration and communication among different teams and companies are essential for successful thermal analysis
  Mesh, node control, and boundary conditions are all extremely important in finding accurate/relevant results

## Slide 13
#9
Setup
  Aluminum facesheet (Al 7075-T6)
  E = 10400 Ksi = psi
  V = 0.33
Parameters
  Height = 1 in.
  Internal Pressure = 23 Psi
  Fracture toughness = 1.6 lb./in.
  FOS = 2.0
    1.6/2.0 = 0.8 lb./in.
Need to cover at least 1,000 ascent cycles
NDE methods can detect a circular flaw size of as little as 0.75 in.
Using closed form solutions shown on the right
  E = modulus
  h = thickness
  a(c) = critical crack length
  P = pressure

## Slide 14
#9
FEA
  Will be using hand calculated thickness of 0.049941 in
  Mesh is made
  23 Psi is applied on the faces-heet

## Slide 15
#9
FEA
  Had an extremely hard time with converging into a solution
  Ran into incrementation issues